## Slide 1: AX85 White Spot SOEM MP Report

## Slide 2
FM65 & FM75 & FM85

## Slide 8
FE75

## Slide 9: Optical performance: Brightness
Properties |  |  | APH75 |  | FE75 DVT |  | FE75 PVT | 
Panel | O-Cell / Spec 5.6% |  | BOE O-mode 5.5% |  | BOE E.mode (n=1) |  | BOE E.mode (n=3) | 
 | Optical Sheet |  | SKC IM334U (MOP) |  | Shinwha 79HMOP-3P |  | Shinwha 79HMOP-3P | 
 | Diffuser Plate |  | EMS-P3 /2T |  |  |  |  | 
 | Backlight If (Ma) |  |  |  |  |  |  | 
LS Bar | LED |  | 3030 2.1∅ Window |  |  |  |  | 
 | Lens |  | 17mm |  |  |  |  | 
Optical | Center Brightness ( Spec >450) | Pure | 453 |  | 458 |  | 488.5 | 
 |  | @Center CIE | 451 |  | 461 |  | 484 | 
 | Color Point |  | 0.2816 | 0.2864 | 0.2758 | 0.2827 | 0.281 | 0.289
 | DCI ( ≥ 92% ) |  | 94.4% |  | 94.3% |  | 93.7% | 
 | Red U’ (>0.49) |  | 0.493 |  |  |  | 0.494 | 
OPT performance spec achieved

## Slide 10: Optical performance: UF/ MURA
FE 75 |  |  |  |  |  |  |  |  | 
Size | 75 |  |  |  |  |  |  |  | 
Package | Nichia 3030 2.5 window size |  |  |  |  |  |  |  | 
Lens | 17mm |  |  | 17mm |  |  | 17mm |  | 
DP | EMS-P3 /2T |  |  | EMS-P3 /2T |  |  | EMS-P3 /2T |  | 
Opt. sheet | Shinwha 79HMOP-3P |  |  | Shinwha 79HMOP-3P |  |  | Shinwha 79HMOP-3P |  | 
CA2000 |  |  |  |  |  |  |  |  | 
Uniformity | 74.25 |  |  | 84.44 |  |  | 82.85 |  | 
Corner Dark | 85% |  | 87% | 85% |  | 83% | 85% |  | 84%
 | Average=89% |  |  | Average=86% |  |  | Average=86% |  | 
 | 89% |  | 93% | 88% |  | 89% | 87% |  | 87%
Mura description | Good but corner dark can be seen a little bit |  |  | Good |  |  | Central part is brighter |  | 
Overall Optical performance achieve target , corner dark is good

## Slide 11
FH75 & FH85

## Slide 12: FH75_Optical performance: Brightness_CSOT
Properties |  |  | FH75 DVT |  | FH75PVT(N=1) |  | FH75PVT(N=2) |  | Production Data Average(N=88) | 
Panel | O-Cell / Spec 5.5% |  | CSOT |  |  |  |  |  |  | 
 | Optical Sheet |  | 79HMOP-3P |  |  |  | SKC (IM334U) |  | Both | 
 | Diffuser Plate |  | EMS-P3 |  |  |  | SANXIN N2 |  | Both | 
 | Backlight If (Ma) |  | 640mA |  |  |  |  |  |  | 
LS Bar | LED |  | SEC |  |  |  |  |  |  | 
 | Lens |  | D127B01 Ø17mm |  |  |  |  |  |  | 
Optical | Center Brightness ( Spec >562) | Pure | 575 |  | 570.09 |  | 531.8 |  |  | 
 |  | @Center CIE | - |  | - |  | - |  | - | 
 | Color Point |  | 0.2756 | 0.2849 | 0.2872 | 0.2958 | 0.2845 | 0.2860 |  | 
 | DCI ( ≥ 95% ) |  | 95% |  | 93.11% |  | 93.62% |  | - | 
 | Red U’ (>0.500) |  | 0.50 |  | 0.500 |  | 0.500 |  | - | 
Line data calibration:
MP specification achieved TGT，2nd vendor performance not achieved
2nd vendor

## Slide 13: FH75_ Optical performance: UF/ MURA
FH 75 |  |  |  |  |  |  |  |  | 
Size | 75 |  |  |  |  |  |  |  | 
Package | SEC |  |  |  |  |  |  |  | 
Lens | D127B01 Ø17mm |  |  | D127B01 Ø17mm |  |  | D127B01 Ø17mm |  | 
DP | SANXIN N2 |  |  | SANXIN N2 |  |  | EMS-P3 |  | 
Opt. sheet | SKC (IM334U) |  |  | SKC (IM334U) |  |  | 79HMOP-3P |  | 
CA2000 |  |  |  |  |  |  |  |  | 
Uniformity | 86.07 |  |  | 86.51 |  |  | 83.71 |  | 
Corner Dark | 79% |  | 78% | 79% |  | 79% | 80% |  | 83%
 | Average=81% |  |  | Average=80% |  |  | Average=83% |  | 
 | 82% |  | 83% | 81% |  | 81% | 83% |  | 84%
Mura description | No obvious Mura occurred |  |  | No obvious Mura occurred |  |  | No obvious Mura occurred |  | 
Mura performance is no problem

## Slide 14: FH85_Optical performance: Brightness_AUO
Properties |  |  | FH85 DVT |  | DVT LINE DATA |  | FH85PVT(N=3) |  | Production Data Average(N=88) | 
Panel | O-Cell / Spec 5.5% |  | AUO |  |  |  |  |  |  | 
 | Optical Sheet |  | SSV QP |  |  |  |  |  |  | 
 | Diffuser Plate |  | EML-R45A |  |  |  |  |  |  | 
 | Backlight If (Ma) |  |  |  |  |  |  |  |  | 
LS Bar | LED |  | LEXTAR |  |  |  |  |  |  | 
 | Lens |  | DA29A Ø17mm |  |  |  |  |  |  | 
Optical | Center Brightness ( Spec >517) | Pure | 534 |  | 529 |  | 538.5 |  | 538.57 | 
 |  | @Center CIE | 513 |  | - |  | 521 |  | - | 
 | Color Point |  | 0.2855 | 0.3008 | 0.2798 | 0.2947 | 0.2894 | 0.2979 | 0.2893 | 0.2998
 | DCI ( ≥ 95% ) |  | 97% |  | - |  | 97.30% |  | - | 
 | Red U’ (>0.500) |  | 0.50 |  | - |  | 0.506 |  | - | 
Line data calibration:
AUO OPT performance is achieved TGT

## Slide 15: FH85_Optical performance: UF/ MURA
FH 85 |  |  |  |  |  |  |  |  | 
Size | 85 |  |  |  |  |  |  |  | 
Package | 3030 |  |  |  |  |  |  |  | 
Lens | DA29A Ø17mm |  |  | DA29A Ø17mm |  |  | DA29A Ø17mm |  | 
DP | EML-R45A |  |  | EML-R45A |  |  | EML-R45A |  | 
Opt. sheet | SSV QP |  |  | SSV QP |  |  | SSV QP |  | 
CA2000 |  |  |  |  |  |  |  |  | 
Uniformity | 90.10 |  |  | 87.55 |  |  | 85.39 |  | 
Corner Dark | 86% |  | 85% | 88% |  | 88% | 88% |  | 88%
 | Average=87% |  |  | Average=89% |  |  | Average=89% |  | 
 | 88% |  | 88% | 90% |  | 91% | 90% |  | 88%
Mura description | No obvious Mura occurred |  |  | No obvious Mura occurred |  |  | No obvious Mura occurred |  | 
Mura performance is no problem

## Slide 16: FH85_ Optical performance: Brightness_INX
Properties |  |  | FH85 DVT |  | DVT LINE DATA |  | FH85PVT(N=3) |  | Production Data Average(N=102) | 
Panel | O-Cell / Spec 5.8% |  | INX |  |  |  |  |  |  | 
 | Optical Sheet |  | SSV QP |  |  |  |  |  |  | 
 | Diffuser Plate |  | EML-R45A |  |  |  |  |  |  | 
 | Backlight If (Ma) |  |  |  |  |  |  |  |  | 
LS Bar | LED |  | LEXTAR |  |  |  |  |  |  | 
 | Lens |  | DA29A Ø17mm |  |  |  |  |  |  | 
Optical | Center Brightness ( Spec >562) | Pure | 550 |  | 552 |  | 548.70 |  | 550.75 | 
 |  | @Center CIE | 531 |  | - |  | 533 |  | - | 
 | Color Point |  | 0.2942 | 0.2985 | 0.2897 | 0.2961 | 0.2942 | 0.2963 | 0.2912 | 0.2942
 | DCI ( ≥ 95% ) |  | 97% |  | - |  | 95.87% |  | - | 
 | Red U’ (>0.500) |  | 0.50 |  | - |  | 0.504 |  | - | 
Line data calibration:
INX OPT performance is same as DVT, confirm the result with S’OEM

## Slide 17: FH85_ Optical performance: UF/ MURA_INX
FH 85 |  |  |  |  |  |  |  |  | 
Size | 85 |  |  |  |  |  |  |  | 
Package | 3030 |  |  |  |  |  |  |  | 
Lens | DA29A Ø17mm |  |  | DA29A Ø17mm |  |  | DA29A Ø17mm |  | 
DP | EML-R45A |  |  | EML-R45A |  |  | EML-R45A |  | 
Opt. sheet | SSV QP |  |  | SSV QP |  |  | SSV QP |  | 
CA2000 |  |  |  |  |  |  |  |  | 
Uniformity | 89.79 |  |  | 90.42 |  |  | 90.73 |  | 
Corner Dark | 85% |  | 86% | 85% |  | 85% | 84% |  | 87%
 | Average=88% |  |  | Average=87% |  |  | Average=87% |  | 
 | 89% |  | 90% | 87% |  | 89% | 84% |  | 91%
Mura description | No obvious Mura occurred |  |  | No obvious Mura occurred |  |  | No obvious Mura occurred |  | 
Mura performance is no problem

## Slide 18
FT75 & FT85

## Slide 19: Optical performance: Brightness
Properties |  |  | FT75 DVT |  | FT75 PVT | 
Panel | O-Cell / Spec 5.6% |  | CSOT 120 Hz |  |  | 
 | Optical Sheet |  | QPP Shinwa [444EPP-LS2] |  |  | 
 | Diffuser Plate |  | Sanxin [GP55-DHK] |  |  | 
 | Backlight If (Ma) |  |  |  |  | 
LS Bar | LED |  | Nichia (FXN) |  |  | 
 | Lens |  | 15.5mm (Enplus) |  |  | 
Optical | Center Brightness ( Spec >730) | Pure | 844 |  | 737.18 | 
 |  | @Center CIE | 829 |  | 725 | 
 | Color Point |  | 0.2872 | 0.2921 | 0.2863 | 0.2915
 | DCI ( ≥ 95% ) |  | 93.5% |  | 93.88% | 
 | Red U’ (>0.510) |  | 0.511 |  | 0.512 | 
Center brightness & DCI didn’t achieve TGT

## Slide 20: Optical performance: UF/ MURA
FT 75 |  |  |  |  |  |  |  |  | 
Size | 75 |  |  |  |  |  |  |  | 
Package | Nichia (FXN) G-Chip 15V |  |  |  |  |  |  |  | 
Lens | 15.5mm (Enplus) |  |  | 15.5mm (Enplus) |  |  | 15.5mm (Enplus) |  | 
DP | Sanxin [GP55-DHK] |  |  | Sanxin [GP55-DHK] |  |  | Sanxin [GP55-DHK] |  | 
Opt. sheet | QPP Shinwa [444EPP-LS2] |  |  | QPP Shinwa [444EPP-LS2] |  |  | QPP Shinwa [444EPP-LS2] |  | 
CA2000 |  |  |  |  |  |  |  |  | 
Uniformity | 90.20 |  |  | 92.49 |  |  | 91.70 |  | 
Corner Dark | 73% |  | 74% | 72% |  | 74% | 75% |  | 72%
 | Average=73% |  |  | Average=74% |  |  | Average=73% |  | 
 | 72% |  | 74% | 74% |  | 75% | 72% |  | 73%
Mura description | No obvious Mura occurred |  |  | No obvious Mura occurred |  |  | No obvious Mura occurred |  | 
OPT performance is OK

## Slide 21: Optical performance: Brightness
Properties |  |  | FT85 DVT |  | FT85 PVT (3PCS AVE) | 
Panel | O-Cell / Spec 5.4% |  | AU0 120Hz |  |  | 
 | Optical Sheet |  | QPP SSV In House |  |  | 
 | Diffuser Plate |  | Entire [EMS-42K7] |  |  | 
 | Backlight If (Ma) |  |  |  |  | 
LS Bar | LED |  | Nichia (FXN) |  |  | 
 | Lens |  | 15.5mm (Enplus) |  |  | 
Optical | Center Brightness ( Spec >730) | Pure | 780 |  | 775.85 | 
 |  | @Center CIE | 767 |  | 780 | 
 | Color Point |  | 0.2843 | 0.2919 | 0.2797 | 0.2827
 | DCI ( ≥ 95% ) |  | 97.8% |  | 97.78% | 
 | Red U’ (>0.510) |  | 0.514 |  | 0.516 | 
OPT performance is OK

## Slide 22: Optical performance: UF/ MURA
FT 85 |  |  |  |  |  |  |  |  | 
Size | 85 |  |  |  |  |  |  |  | 
Package | Nichia (FXN) G-Chip 15V |  |  |  |  |  |  |  | 
Lens | 15.5mm (Enplus) |  |  | 15.5mm (Enplus) |  |  | 15.5mm (Enplus) |  | 
DP | Entire [EMS-42K7] |  |  | Entire [EMS-42K7] |  |  | Entire [EMS-42K7] |  | 
Opt. sheet | QPP SSV In House |  |  | QPP SSV In House |  |  | QPP SSV In House |  | 
CA2000 |  |  |  |  |  |  |  |  | 
Uniformity | 86.6 |  |  | 84.5 |  |  | 88.7 |  | 
Corner Dark | 85% |  | 83% | 82% |  | 81% | 81% |  | 82%
 | Average=84% |  |  | Average=83% |  |  | Average=82% |  | 
 | 84% |  | 85% | 85% |  | 84% | 82% |  | 83%
Mura description | No obvious Mura occurred |  |  | No obvious Mura occurred |  |  | No obvious Mura occurred |  | 
OPT performance is OK

## Slide 23: Timeline
 | 2022 |  |  |  |  |  |  |  |  | 
 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11
B/C Prod |  |  |  |  |  |  |  |  |  | 
B/C SBI |  |  |  |  |  |  |  |  |  | 
Pmod Prod |  |  |  |  |  |  |  |  |  | 
FT-IR |  |  |  |  |  |  |  |  |  | 
White Spot |  |  |  |  |  |  |  |  |  | 
7/3
9/11
ESON
9/27
SSVE 0/144pcs
outsource to 3rd Party
ESON
SSVE
11/1
10/8
SSVE Rework
0/204pcs
10/29
SSVE 0/300pcs
9/27
SOEM Line -> SBI
10/29
FSK, SBI: 20/289pcs
SSVE 0/270pcs
10/29
TODAY

## Slide 24: LCM History & Package @SSVE
Pmod History
No repair;
Process timetable is continuous(direct output);
HUB_OUT_DATE | TOPLACES | PART_NO | PLT_ID | CTR_NO | PART_NO_SERIALNO
12/4/2021 | SOEM | A5027725A | SSVE21M3460101 | SUDU8846144 | A5027725A$0037447
12/4/2021 | SOEM | A5027725A | SSVE21M3460101 | SUDU8846144 | A5027725A$0037448
12/4/2021 | SOEM | A5027725A | SSVE21M3460101 | SUDU8846144 | A5027725A$0037449
12/4/2021 | SOEM | A5027725A | SSVE21M3460101 | SUDU8846144 | A5027725A$0037450
12/4/2021 | SOEM | A5027725A | SSVE21M3460101 | SUDU8846144 | A5027725A$0037451
12/4/2021 | SOEM | A5027725A | SSVE21M3460101 | SUDU8846144 | A5027725A$0037452
12/4/2021 | SOEM | A5027725A | SSVE21M3460101 | SUDU8846144 | A5027725A$0037453
12/4/2021 | SOEM | A5027725A | SSVE21M3460101 | SUDU8846144 | A5027725A$0037454
12/4/2021 | SOEM | A5027725A | SSVE21M3460101 | SUDU8846144 | A5027725A$0037455
12/4/2021 | SOEM | A5027725A | SSVE21M3460101 | SUDU8846144 | A5027725A$0037456
12/4/2021 | SOEM | A5027725A | SSVE21M3460101 | SUDU8846144 | A5027725A$0037457
12/4/2021 | SOEM | A5027725A | SSVE21M3460101 | SUDU8846144 | A5027725A$0037458
Pmod Package Section View(Face5): LIFO
12
1
2
3
4
5
6
Face4
Face2

## Slide 25: Mech: Package & Structure vs Glass Broken
Pmod Package Structure
 There is no coverage by cushion at the broken area;
Pmod structure shows
 There is no support pin near the broken area;

## Slide 26: SEA Freight
(SSVE – FSK) = (SSVE – SOEM) + (SOEM – FSK)
(SSVE – SOEM) : ?=?
(SSVE – FSK ) : ?=?
(SOEM – FSK)
(SSVE – SOEM)

## Slide 27: Temp. && Humidity in Pallet
 | From | Pmod Carton Temp. In Container | To SOEM
Process | SSVE |  | 
Chart: Temperature[C] Inside Bag(SSVE->SOEM)
Chart: Temperature[C] Outside Bag(SSVE->SOEM)
▲ Source: provided by HESC-Mech, 2020
Temp.(℃) | min | max | average | Δ
outside-bag | 22.1 | 29.6 | 25.3 | 7.5
inside-bag | 22.4 | 32.8 | 27.0 | 10.4
Hum.(%) | min | max | average | Δ
outside-bag | 65.2 | 80.7 | 75.1 | 15.5
inside-bag | 61.1 | 76.1 | 69.8 | 15.0

## Slide 28: Mura & OD
指摘品 | 0H(CST 13:20) | 1H(CST 14:20) | 2H(CST 15:20)
100IRE |  |  | 
50IRE |  |  | 
OD |  |  | n.a
(1, 2)
(1, 1 )
(1, 1 )
(0.5, 1.5)
(0, 0 )
(1, 0.5)
(1, 1,5)
(1, 1)
(1.5, 1 )
(横方向ギャップ, 縦方向ギャップ)
-1mm
-1mm
(1, 1)
(1, 1 )
(1.5, 1 )
(0.5, 1)
(0, 0 )
(1, 0.5)
(1, 1,5)
(1, 1)
(1, 1 )
(横方向ギャップ, 縦方向ギャップ)
-1mm
-1mm
DP
ALF
OCell中心凸
OCell中心凸

## Slide 29: CHN Market | LENS Mura | ITU-R
Room Temp. | 0H | 2H | 4H | 6H
Ser. 1505498 |  |  |  | 
LENS Mura | ITU-R=4.0 | ITU-R=4.0 | ITU-R=4.0 | ITU-R=4.0
Extra Op. | n.a |  |  | n.a
After pushed OCell Center, LENS Mura doesn’t change
Face 2 Upward, Twist, 3x
Face 2 Center, Push, 3x
Hold
Push

## Slide 30
MURA | 0H | 1H | 1H, After tap, 0min | 1H, After tap, 2min
OFF |  |  |  | 
ON |  |  |  | 
AG65 SET | 50IRE | Mura ON/OFF
ITU-R=3.5
ITU-R=3.5
ITU-R=5.0
ITU-R=3.5
ITU-R=4.0
ITU-R=4.0
ITU-R=5.0
ITU-R=4.0
B/C tapping
⇒It’s suspected that Mura correction data was corresponding with OD SSVE product line;
⇒It’s suspected that after SSVE shipment, OD worsened due to transportation and vibration, Mura correction data became insufficient;

## Slide 31: DP Warpage | Original DP + New BC/LS/Ref
 | 0H(CST 10:45) | 0.5H(CST 11:15) | 1H(CST 11:45)
指摘品DP |  |  | 
(5.5, 5)
(7, 6 )
(6, 5 )
(5, 5)
(8, 8)
(4, 4.5)
(5, 6)
(7.5, 7)
(4.5, 5 )
(横方向ギャップ, 縦方向ギャップ)
+2.4mm
+2.5mm
(6. 5)
(7, 6)
(5.5, 5 )
(6, 5)
(10, 9)
(4, 5)
(5, 5)
(7, 7)
(5, 5.5 )
(横方向ギャップ, 縦方向ギャップ)
+4.3mm
+3.5mm
DP
ALF
DP中心凹み
DP中心凹み
(6, 5)
(7, 6)
(6, 5 )
(6, 5)
(10, 9)
(4, 4)
(5.5, )
(7, 7)
(5, 6 )
(横方向ギャップ, 縦方向ギャップ)
+4.3mm
+3.5mm
DP中心凹み
指摘品DP + 新BC/LS/Ref, 中心凹み量は4mmです。
OD悪化は再現した。 ⇒DP自体が悪い

## Slide 32: Transportation Summary
 | SSVE::LCM Package | ETD::SSCS Loading | Shipment::Boat | Input::FSK SET Line
SSVE21S4210090 | OK: followed SOP | OK: no error found |  | 
SSVE21S4210101 | OK: followed SOP |  |  | 
SSVE21S4210070 | OK: followed SOP | OK: no error found |  | 
Conclusion
1. broken origin occurred at one position: Face2, (48.5, 12);
2. SSVE LCM package operation followed SOP, OK;
3. SSCS Loading operation had no wrongdoing found;
=> It assumed that carton pallets got serious external impact when the carton pallets were taken out from containers
carton PLT/Cushion OK
carton PLT/Cushion OK
carton PLT/Cushion OK

## Slide 33: Mech: Pallet Package vs Glass Broken
88.5
178
238
95
299
814
260
48.5
12
Pmod Package Structure
 There is no coverage by cushion at the origin glass broken(48.5, 12);

## Slide 34: Mech Mapping: SP vs Glass Broken
48.5
12
Pmod structure shows
 There is a support pin near the origin of glass broken(48.5, 12)

## Slide 35: Optical Sheet Structure
Capillarity
normally, if oil or water contacts with prism layers, oil or water permeate from edge to inner linearly;
because cohesive and adhesive forces that causes water and other liquids to rise in thin tubes or other constricted spaces;
(Rear view)AX85 QOP Sheet, white spot
TOP
BTM
AX85 QOP

## Slide 36: DP Structure
DP
QOP
OCell
DP(R45), surface moire: Vertical

## Slide 37: Dew Test
Chamber #1
FSK仕様x1p
SOEM仕様x1p
Chamber #2
FSK仕様x1p
SOEM仕様x1p
Temp. = 50℃
Hum. = 70%
Duration = 5H
Pmod = OFF
Temp. = 0℃
Hum. = 70%
Duration = ∞H
Pmod = ON(auto) per confirm
Confirm = 1 time per 24H
Face2
Face4
Pmod Package Section View(Face6): FIFO
12
1
2
3
4
5
6
9
Face2
Face4
Pmod Package Section View(Face6): FIFO
12
1
2
3
4
5
6
9

## Slide 38: Package Mapping: Pmod Package Sequence
Pmod Package Section View(Face5): FIFO
12
12685
HIS_DATE | PRODUCTIONID | ITEM_NAME | PALLETID | TOWHSCD | SERIALNO | CARTONNO
9/7/2021 11:32 | A5027713A | AX85 | SSVE21S3310088 | SOEM | 12679 | MOFU6750614
9/7/2021 11:32 | A5027713A | AX85 | SSVE21S3310088 | SOEM | 12680 | MOFU6750614
9/7/2021 11:32 | A5027713A | AX85 | SSVE21S3310088 | SOEM | 12681 | MOFU6750614
9/7/2021 11:32 | A5027713A | AX85 | SSVE21S3310088 | SOEM | 12682 | MOFU6750614
9/7/2021 11:32 | A5027713A | AX85 | SSVE21S3310088 | SOEM | 12683 | MOFU6750614
9/7/2021 11:32 | A5027713A | AX85 | SSVE21S3310088 | SOEM | 12684 | MOFU6750614
9/7/2021 11:32 | A5027713A | AX85 | SSVE21S3310088 | SOEM | 12685 | MOFU6750614
9/7/2021 11:32 | A5027713A | AX85 | SSVE21S3310088 | SOEM | 12686 | MOFU6750614
9/7/2021 11:32 | A5027713A | AX85 | SSVE21S3310088 | SOEM | 12687 | MOFU6750614
9/7/2021 11:32 | A5027713A | AX85 | SSVE21S3310088 | SOEM | 12688 | MOFU6750614
9/7/2021 11:32 | A5027713A | AX85 | SSVE21S3310088 | SOEM | 12689 | MOFU6750614
9/7/2021 11:32 | A5027713A | AX85 | SSVE21S3310088 | SOEM | 12690 | MOFU6750614
1
2
3
4
5
6
Face4
Face2

## Slide 39: Fishbone
>>> Ongoing

## Slide 40: Failure Mode && Risk
 | Y-axis view | X-axis view | Factors | Market Risk
OK |  |  | - | -
Failure mode1 |  |  | x or y, direction | high
Failure mode2 |  |  | x or y, direction | high
Failure mode3 |  |  | z-axis, pressure | low (SSVE can detect)
x
y
z
L
R
BTM
TOP
L
R
BTM
TOP
L
R
BTM
TOP
L
R
BTM
TOP
interdependent relationship
previous LED fail
WK48 LED fail, 4pcs
WK48, 4pcs

## Slide 41: SBI Result
AX75 before WK50, 800pcs, GIL(II)=J
Sample size = 125, Ac=0, Re=1
 | Ac | Re
0 | 0.284708 | 0.715292227
1 | 0.644187 | 0.355812715
2 | 0.869316 | 0.130684132
3 | 0.962551 | 0.037449062
4 | 0.991275 | 0.008725127
5 | 0.998296 | 0.00170372
SBI Result @SOEM
No | Date | Model | Ok | Ng
1 | 1/8/2022 | YDBM075CCS02 | 96 | 0
2 | 1/9/2022 | YDBM075CCS02 | 96 | 0
3 | 1/10/2022 | YDBM075CCS02 | 276 | 0
According to SONY AQL standard,
the current SBI result proved the lots are safe and acceptable;
Chart: OC Curve
| 0 | 0.01 | 0.02 | 0.03 | 0.04 | 0.05 | 6.0000000000000005E-2 | 7.0000000000000007E-2 | 0.08 | 0.09 | 9.9999999999999992E-2 | 0.10999999999999999 | 0.11999999999999998 | 0.12999999999999998 | 0.13999999999999999 | 0.15
Reject | 1 | 0.64419 | 0.28419 | 0.10805 | 0.037747 | 0.012447 | 0.0039282 | 0.0011961 | 0.00035311 | 0.00010141 | 2.8391e-05 | 7.7607e-06 | 2.0735e-06 | 5.4186e-07 | 1.3857e-07 | 3.469e-08

## Slide 42: White Line History

## Slide 43: 2019, SL85
SL85 Oil remaining picture
SL85 Symptom : White line from BC touch position

## Slide 44: No1 NX85, Whiteline, SN0008764
視角 | 写真
正面： 見ずらい、写真取れない | 
斜め： はっきり見える | 
S O N Y
L = 23
L=19
L=10
L=11
L = 21
L1= 20
H=1.5
L=2.5
①
②
Item | Details
PMOD | NX85
Locality | SOEM
DateTime | 20200914
Symptom | WhiteLine
Q’TY | 4pcs
R/C | TBD
C/M | TBD
Whitelineの位置を確認し、長さ測定し、該当パネルのTOP HOOKから発生したと思われます。
正面視、見ずらいです、写真取れない
斜めから見える

## Slide 45: 光学シート
箇所 | 光学シート耳(裏面、左) | 光学シート耳(裏面、右)
OK |  | 
① |  | 
② |  | 
視角 | 写真
正面： 異常なし | 
裏面： はっきり見える | 
重い
重い
重い
軽い
Whitelineの位置、形状は光学シート裏面にある異物の位置と合っている
10X

## Slide 46: REF & BC
WhiteLineの位置と応じるB/Cには、油ぽいことが発見した
WhiteLineの位置と応じるREF裏面には、油ぽいことが発見した
10X
宿題：
異物の本体は何でしょうか ⇒ 成分分析
異物はどうやって侵入したか ⇒ 模擬テスト

## Slide 47: 5W2H Template (Simple Cases)
5W2H | Statement | Status | Date
What? |  |  | 
Who? |  |  | 
Where? |  |  | 
Why? |  |  | 
When? |  |  | 
How? |  |  | 
How Much? |  |  | 
Comments: |  |  | 
Note: MSA and Gage R&R are basic and essential

## Slide 48: Fishbone Template (Moderate Cases)
Note: Product and Process understanding are critical

## Slide 49: 8D Template (Complicated Cases)
2D
3D
4D
5D
1D
8D
7D
6D
Define
Team
Describe Problem
Develop Containment Plan
Determine and Verify Root Causes
Verify Permanent Solutions
Implement
Corrective Actions
Prevention
Congratulate the team
Note: TQM and QC tools are important

## Slide 50: 8D Template
Team
Problem
Containment Plan
Root Cause
Permanent Counter Measures
Corrective Actions
Prevention
Check Effectiveness
Note: picture first, numbers second

## Slide 51: Conclusion
TV Plant | Q’TY(pcs) | Bracket Supporter Broken | Ratio(Dppm)
CTTI | 10,609 | 0 | 0
FSK | 32,560 | 0 | 0
SOEM | 36,217 | 1 | 28
China Market | 44,720 | 0 | 0
TTL | 124,106 | 1 | 8
Bracket support broken
OR
Part
Assy
Assy WWOPS
Inspection OPS
part performance
assy
performance
x
Inspection
enhancement
Impact
Low
High
Low
High
ALF
supporter
Bracket
Likelihood
Insp.
OPS
Assy

## Slide 52
E.O.F